## Slide 1: Exploring second-order Nonlinear optics in mono- and few-layer 2D perovskites
Himal Oli
Steve Smith
Tula R. Paudel
Workshop for AI-Powered Materials Discovery at Great Plains University of South Dakota
June 24, 2025

## Slide 2: Research overview
Background
Why 2D Perovskites?
Types of 2D Perovskites
Basics of Second-Order Nonlinear Optics
My work on Perovskites
Future Prospects
Summary

## Slide 3: Background
In 1978, the first synthesis of organic-inorganic lead halide perovskite
In 1892, the first synthesis of a cesium lead halide perovskite
Named after the Russian mineralogist Lev Perovski
Discovered by German mineralogist Gustav Rose in 1839
Perovskites
The mineral is based on calcium titanate ()
In 1986, the first layered perovskite reported
In 2009, Tsutomu Miyasaka et al. reported the first incorporation of perovskite materials into a solar cell
Mahapatra et al., Intro to Perovskite, Springer, 2024.

## Slide 4: Why 2D Perovskites?
Strong quantum confinement enhances nonlinear optical response
Enhanced light-matter interactions
High χ² (second-order susceptibility) values due to low-dimensional structure and strong excitonic effects
Potential for miniaturized and flexible photonic devices
Tunable optical properties via compositional engineering
Ultrafast photonic responses
N
Pb
Br
C
H
Crystal structure of 2D Perovskite
https://www.ossila.com/pages/what-are-2d-perovskites

## Slide 5: Types of 2D Perovskites
Types of 2D perovskites:
Ruddlesden-Popper: Alternating layers of perovskite and organic spacers
Dion-Jacobson: Similar to Ruddlesden-Popper but without A-site cations
Aurivillius: Typically found in oxide perovskites with alternating oxide layers
Figure: Representative structures of perovskite and layered perovskites: (a) cubic-SrTiO3 with simple perovskite structure, (b) CsLaNb2O7 with n = 2 D–J structure, (c) Sr3Ti2O7 with n = 2 R–P structure, and (d) T-Bi2SrTa2O9 with n = 2 Aurivillius structure.
Influence of structure on optical and electronic properties
B. H. Zhang et al., J. Phys. D: Appl. Phys. 55, 113001 (2022).

## Slide 6: Basics of Second-Order Nonlinear Optics
Second-harmonic generation (SHG): Doubling of photon frequency
Mathematical expression representing second-order susceptibility (χ²)
Requires non-centrosymmetric materials for a non-zero χ²
https://gibbs.chem.ualberta.ca/?p=9

## Slide 7: Step by Step of a Mechanical Exfoliation Process
Mechanical Exfoliation

## Slide 8: Optical Microscope Images of Exfoliated 2D flake on Glass Substrate
Notes: AI can be used to

## Slide 9: EDS/SEM Elemental Analysis of 2D
Element | Atomic % | Atomic % Error | Weight % | Weight % Error | Net Counts
N | 21.5 | 0.9 | 18.9 | 0.8 | 10 117
Pb | 0.9 | 0.2 | 11.4 | 2.0 | 3 182
C | 74.9 | 0.4 | 56.2 | 0.3 | 112 502
Br | 2.7 | 0.3 | 13.6 | 1.3 | 4 250

## Slide 10: XRD Pattern of 2D

## Slide 11: Band Plot of 2D
Vienna Ab initio Simulation Package (VASP) for Density Functional Theory (DFT) calculations

## Slide 12: DOS plot of 2D
Orbital-resolved DOS plot of 2D (Benzylammonium)2 PbBr4 Perovskite
Atom-resolved DOS plot of 2D (Benzylammonium)2 PbBr4 Perovskite

## Slide 13: Crystal structure and band plot of monolayer 2D

## Slide 14: Crystal structure showing atom displacement and dos plot of C-atom of monolayer 2D
C

## Slide 15: Crystal structure of bilayer 2D

## Slide 16: Band and atom-resolved dos plot of bilayer 2D

## Slide 17: Band and atom-resolved dos plot (dipole correction) of bilayer 2D

## Slide 18: Comparison of Potential Profile of 2D Perovskite

## Slide 19: Future Prospects
Future directions:
AFM will be used to quantify nanosheet thickness
Raman spectroscopy and TEM will provide insight into phonon modes, crystallinity, and structural integrity
SHG will be performed to probe the nonlinear optical properties and emission characteristics of these materials
Second-order susceptibility will be calculated theoretically to complement the experimental findings
Future work will extend these investigations to chloride and iodide analogues

## Slide 20: AI in 2D Perovskite-Based Nonlinear Optics
Current Challenges:
  Thickness-dependent optical nonlinearity
  Limited high-throughput prediction of second-order susceptibility
AI/ML:
  AI-driven deep learning enables automated, accurate identification of mono- and bilayers from microscopy images, streamlining flake isolation without damage (Yu Saito et al., 2019)
  Machine learning models trained on computational 2D materials databases (C2DB) have predicted second-order susceptibility χ², accelerating nonlinear material screening (Haastrup et al., 2018)
Notes: The nonlinear optical response is highly sensitive to the number of layers. Isolating mono- and bilayers without damaging the sample or altering its structure presents a fabrication and reproducibility challenge.
This allows rapid computational screening to identify promising candidate materials without performing full DFT/BSE calculations.

## Slide 21: Summary
Mechanical exfoliation technique was used to exfoliate the bulk crystals to few-layered nanosheets.
Characterization techniques like XRD, and EDS/SEM confirmed the crystal structure, elemental composition, and morphology, verifying the high quality and purity of the sample.
Electronic properties were explored through band structure analysis and density of states.
Atom- and orbital-resolved density of states revealed the contributions from lead and halide orbitals.
The additional band(s) near 2 eV in the monolayer and bilayer originated from surface carbon atoms.

## Slide 22: Acknowledgments
Special thanks to:
Dr. Tula R. Paudel
Dr. Steve Smith
Dr. Alexey Lipatov and his lab
Mr. Khimananda Acharya

## Slide 25: XRF

## Slide 26: Dos plot of C-atom of monolayer 2D