## Slide 1
Emerging AI tools for controlling grain structure, phases, and defects in
3D printed metallic parts
Metal 3D printing: uniqueness and opportunities
Need to control grains, phases, and defects
Why AI?
Several applications
Future perspectives
Tuhin Mukherjee
Mechanical Engineering, Iowa State University
Workshop for AI-Powered Materials Discovery at Great Plains University of South Dakota, 23 June 2025
Contents:
T. Mukherjee, Welding Journal, 2024.

## Slide 2
Metal printing: uniqueness and opportunities
3D printing in space (NASA)
DebRoy, Mukherjee, Milewski et al. Nature Materials. 2019
Only a handful of over 5,000 commercial alloys are printed
Failure to control structure, properties, and defects

## Slide 3
Main challenges: controlling grains, phases, & defects
Lack of fusion voids
Xia et al. Int. J Machine Tool. Manuf. 2017
Surface roughness
Cao et al. Add. Manuf. 2021
Structure
Defects
Properties
Hardness variation
Mukherjee et al. Acta Mater. 2021
Columnar grains
Equiaxed grains
Todaro et al. Nature Comm. 2020

## Slide 4
Why artificial intelligence?
Important variables: laser power, scanning speed, laser beam radius, layer thickness, preheat temperature, hatch spacing, substrate dimensions, specific heat, thermal conductivity, density, solidification range, Youngs modulus.
Minimum experiments needed:
212 (=4096) - 2-factor DOE
AI tools can help reduce the parameter space, minimize trial-and-error, and improve quality

## Slide 5
Machine learning
Problem type
Examples
Machine learning algorithms
Regression problems
Classification problems
Control of geometry, grain size, residual stress, distortion
Control of defect formation, solidification morphology
Linear regression, neural network, Bayesian network
Decision tree, random forest, support vector machines

## Slide 6
Physics-informed machine learning
Heat source
Mirror
Powder spreader
Roll
Substrate
Powder bed
Part
Benefits
Calculates variables that affect structure, properties, and defects
Provides scientific insights
Guides experiments by selecting appropriate process conditions
Machine learning
Mechanistic modeling
Additive manufacturing experiments
Benefits
Does not need phenomenological understanding
Reliable prediction with less data
Hierarchical importance of variables

## Slide 7
Deep learning
Sample number
Variable
Parameter 1
Parameter 2
(b) Printed part
(c) CT image of part
CT images capture the defect formation
(d) Raw data distribution
Deep learning results support experiments
(e) Deep learning results
(a) AM process
Adapted from Yao et al. JMSE, 2018
Can handle large dataset

## Slide 8
1. Control of grain structure using machine learning
AM process model &
3D kinetic Monte Carlo grain growth model
Ongoing work at
Iowa State University

## Slide 9
Control of grain structure using machine learning
DebRoy, Mukherjee, Wei et al. Nature Reviews Materials. 2021
The grain growth is computed using a Monte Carlo model.
Grain size versus frequency data in longitudinal and transverse directions
These data are used to train a neural network that could then calculate grain growth
Khanzadeh et al. SMEJMP. 2018

## Slide 10
2. Hardness control using physics-informed ML
Hardness of ferritic steels parts are affected by martensite
Repeated heating and cooling during multilayer deposition tempers martensite
CCT diagram of Grade 91 ferritic steel
Mukherjee et al. Acta Materialia. 2021
Mukherjee et al. J Manufacturing Processes. 2022

## Slide 11
The physics-informed machine learning framework
Neural network
Input
Hidden layer
Output
Heat transfer and fluid flow model
Isothermal tempering data
Calculated thermal cycles
Accurately calculated thermal cycle
Tempering data from literature
Process conditions and alloy properties
JMA constants
Hardness of the part
JMA: Johnson Mehl Avrami equation

## Slide 12
Predicted tempering and hardness
Mukherjee et al. J Manufacturing Processes. 2022

## Slide 13
3. Machine learning to reduce lack of fusion
LFI = 0.473 H – 0.15 D – 2.61 × 10-5Ma – 0.122 T + 0.306 Fo + 0.569
H : Dimensionless hatch spacing
D : Dimensionless pool depth
Ma : Marangoni number
T : Dimensionless peak temperature
F0 : Fourier number
Jiang, Mukherjee et al. npj Computational Materials. 2022

## Slide 14
Hierarchy of variables affecting lack of fusion
D > H > Ma > T >F0
Hierarchical importance
Dimensionless hatch spacing, H
(Hatch spacing/Pool width)
Dimensionless pool depth, D
(Pool depth/Layer thickness)
Marangoni number, Ma
Dimensionless peak temperature, T
(Peak temperature/Liquidus temperature)
Fourier number, F0
Jiang, Mukherjee et al. npj Computational Materials. 2022

## Slide 15
4. Calculation of residual stress to train ML
Inconel 718
Stainless steel 316
Ti-6Al-4V
Mukherjee, DebRoy, STWJ, 2019
Mukherjee, Zhang, DebRoy, Comput. Mater. Sci. 2017.
Different processes
Different materials
DED-L

## Slide 16
Prediction and control of residual stress
Computed residual stress values were used for training.
Based on 243 datasets of 3 alloys SS 316, IN 718 and 800H
Wu, Mukherjee, De et al. Additive Manufacturing. 2020

## Slide 17
5. Distortion control using deep learning
(a) Printed part
(b) Process parameters
(c) Feedstock properties
(d) Temperature field images captured by a pyrometer
(e) 3D distortion of the part predicted by deep learning
Adapted from
Francis et al.
Manufacturing Letters, 2019

## Slide 18
Can ChatGPT etc. help?

## Slide 19
Future perspective: Digital twin of 3D printing
Mukherjee et al. Applied Mater. Today 2019

## Slide 20
Future perspective: Need for quantum computing
IBM Qiskit
Quantum Computer
IBM: Quantum computing is expected to help develop breakthrough products and services that will disrupt and redefine manufacturing
https://www.ibm.com/thought-leadership/institute-business-value/report/quantum-manufacturing
SBIR: Small Business Innovation Research in the US has recently emphasized the importance of quantum computing in 3D printing
https://www.sbir.gov/node/1863263
qiskit.org

## Slide 21
Future perspective: AI-guided materials discovery for AM
Yu et al. Journal of
Materials Informatics, 2021
Designing biocompatible titanium alloys with specific mechanical properties.
Young's modulus (E), martensite start temperature (Ms), and beta phase stability (βLow)
Similar approach can find new printable alloys

## Slide 22
Future perspective: Large language models for AM
RAG: Retrieval Augmented Generation; NER: Named Entity Recognition
Liu et al., RCIM, 2025.

## Slide 23
Summary
Artificial intelligence (AI) tools are useful for controlling microstructure, properties, and defect formation during additive manufacturing.
Availability of several well-tested algorithms and open-source codes allows everyone to use AI.
AI tools can reduce the process parameter space to explore, minimize time-consuming trial-and-error, and improve quality.
Use of digital twins, quantum computing, and large language models can strengthen this field

## Slide 24
Recent contributions and further details

## Slide 25
Thank you!
Tuhin Mukherjee
Assistant Professor
Mechanical Engineering
Iowa State University
tuhinm@iastate.edu
+1 (515)-294-8911