## Slide 1
Advancing Fe-Ga Magnetic Alloys: Synthesis and Theory of Disordered and Ordered Phases
June 24, 2025
Workshop for AI-Powered Materials Discovery at Great Plains
Connor McCollar
1

## Slide 2
Overview of Presentation
MANC briefing and research aims
Experimental aspects of the research
  Ribbon fabrication and characterization
Theoretical/computational aspects of the research
  Utilization of machine learning in studying disordered phase
2
6/24/2025

## Slide 3
MANCs Background
Metallic amorphous matrix
Nanocrystalline grains
MANC – Metal Amorphous Nanocomposite
  Composed of both amorphous and crystalline phases
3
6/24/2025

## Slide 4
MANCs Background cont.
MANC – Metal Amorphous Nanocomposite
  Composed of both amorphous and crystalline phases
Important properties of MANCs:
  Distinct magnetic properties: soft magnetism & relatively large saturation magnetization
Applications
  Inductor cores, energy storage
M
H
M
H
Hysteresis loop of soft magnet.
Hysteresis loop of hard magnet.
4
6/24/2025

## Slide 5
Research Aims
Explore alternative composition to commercial FINEMET
  FINEMET composition: Fe-Nb-Cu-Si-B
  Our composition swapping Si for Ga: Fe-Nb-Cu-Ga-B
Study the properties of Fe-Ga alloys
Utilize Machine-Learned force fields (MLFFs) for studying disordered systems
Long term: Produce Fe-Ga MANC with optimal magnetic properties
5
6/24/2025
Notes: The main goals of this research project are:
Explore alternative composition MANC from the commercially available FINEMET MANC.
We want to produce an iron-gallium based MANC in the lab
We want to study it’s properties (magnetic and structural) since FINEMET properties come in part from very small nanocrystals in the amorphous matrix

## Slide 6
Fabricating Amorphous Alloys
Prevent atoms from arranging into ordered structure
  Prepare ingots with desired composition by arc melting
  Rapidly cool and spin out into thin ribbon (~20μm thick)
Ingot of alloy produced by arc melting.
Laboratory arc melter.
6
6/24/2025

## Slide 7
Fabricating Amorphous Alloys cont.
Ribbon being produced at NASA Glenn Research Center (NASA).
Laboratory melt-spinner.
Prevent atoms from arranging into ordered structure
  Prepare ingots with desired composition by arc melting
  Rapidly cool and spin out into thin ribbon (~20μm thick)
7
6/24/2025

## Slide 8
Characterizing Fe-Ga Alloys
Studying structural properties
  Tools: X-ray diffraction, TEM/Selected Area Electron Diffraction (SAED)
Studying magnetic properties
  Tools: Vibrating sample magnetometer (VSM)
Important experimental step in studying the properties of the materials
8
6/24/2025

## Slide 9
Determination of Crystalline Alloy by XRD
Bragg’s Law
– distance between crystal planes
– angle of incident X-rays
2 possible crystalline phases of Fe-Ga:
Ordered Fe3Ga
Disordered Fe4Ga
(1 1 0)
(2 2 0)
(2 0 0)
(4 0 0)
(2 1 1)
(4 2 2)
or
or
or
9
6/24/2025
Notes: d tells us about the structure of the material
Theta we use to determine d. Tells us about the structure of the materials
Given all the correct measurements, we can quite determine the exact plane & crystal structure. With our methods of fabrication, this is difficult we form polycrystalline material and can’t reduce samples to powder.
A. Factors like sample height displacement and instrument misalignment can cause a systematic shift in the absolute peak positions (2θ values). However, these factors generally don't affect the relative distances between the peaks, making relative peak distances more reliable for structural analysis and phase identification.

## Slide 10
TEM and Selected Area Electron Diffraction
TEM image (left) and SAED pattern (right) for the 1 1 0 zone axis of single crystal in a sample of Fe73.5Nb3Cu1Ga16.5B6 alloy (Paul White).
10
6/24/2025

## Slide 11
TEM and Selected Area Electron Diffraction
SAED pattern for 1 1 0 zone axis of recent sample exhibiting signs of both the ordered Fe3Ga and disordered Fe4Ga phases.
11
6/24/2025

## Slide 12
VSM Results
Magnetometry performed at SDSU
Relatively wide hysteresis loops
Suspected Fe4Ga with significantly increased saturation magnetization
Overlaid Hysteresis Loops for Alloys of Varying Ga Concentration
12
6/24/2025

## Slide 13
Composition | Ms (emu/gm)
Fe-Nb3Cu1Ga13.5B9 | 156
Fe-Nb3Cu1Ga14B8.5 | 158
Fe-Nb3Cu1Ga14.5B8 | 136
Fe-Nb3Cu1Ga15B7.5 | 179
Fe-Nb3Cu1Ga15.5B8 | 162
Fe-Nb3Cu1Ga16B8.5 | 148
Fe-Nb3Cu1Ga16.5B9 | 153
VSM Results cont.
Comparison of Saturation Magnetizations of Alloys of Varying Ga Concentration
13
6/24/2025

## Slide 14
DFT Results on Each Phase
Magnetization: 2.29 μB/atom Fe
Energy: -7.22 eV/atom
Fe4Ga
Magnetization: 2.07 μB/atom Fe
Energy: -7.02 eV/atom
Fe3Ga
Performed Density Functional Theory (DFT) calculations with VASP
  Fe3Ga cell containing 16 atoms (12 Fe)
  Fe4Ga special quasirandom structure (SQS) cell containing 54 atoms (43 Fe)
Magnetization and energy per atom of each phase determined to be:
14
6/24/2025

## Slide 15
Completed Work
Fabricated ribbons of Fe-Ga alloy
Characterized the structural and magnetic properties of alloy
  XRD determined none were amorphous—possibility of either ordered Fe3Ga and disorder Fe4Ga states
  TEM/SAED confirmed presence of Fe4Ga
  VSM found large magnetization values for Fe4Ga alloy
Used DFT to verify results with theory
  Found Fe4Ga to have higher magnetization in agreement with VSM
15
6/24/2025

## Slide 16
16
6/24/2025
How will machine learning influence this research?

## Slide 17
VASP Machine Learning Force Fields
Goal: Build a machine learning force field to explore the composition and configuration spaces of disordered phase
Machine Learning Force Fields (MLFFs)
  Ab initio calculations with DFT & machine learning enable finding force fields for given system
On-the-fly learning
  Suited well for efficiency in choosing training data
17
6/24/2025

## Slide 18
MLFF Training
Disordered system training accomplished by use of many starting SQSs of appropriate composition
Compiled training data of structures
Produce MLFF and/or perform on-the-fly training for improved MLFF
18
6/24/2025

## Slide 19
Acknowledgements
Dr. Tula R. Paudel and Paul White
SDSU for VSM measurements and use of INNOVATOR cluster
NASA EPSCoR
19
6/24/2025

## Slide 20
Thank you for listening!
Contact me: connor.mccollar@mines.sdsmt.edu
All questions and comments are appreciated.
20
6/24/2025