## Slide 1
  Transforming Polymer R&D with AI
Chiho Kim
School of Materials Science and Engineering, Georgia Institute of Technology
Workshop for AI-Powered Materials Discovery at Great Pains 1:30-2:05 PM CDT, Jun 23, 2025, University of South Dakota

## Slide 2: Credits
Ramprasad Research Group at Georgia Tech
Collaborators (GT): Ryan Lively, Blair Brettmann, Will Gutekunst, M. G. Finn, Jerry Qi, Natalie Stingelin, Mark Losego, Valeria Milam, Roshan Joseph, Chao Zhang / Collaborators (UConn): Greg Sotzing, Yang Cao
Matmerize, Inc.
Co-Founder: Rampi Ramprasad (Georgia Tech)
Advisors: Jonathan Goldman (Georgia Tech); Bill Midgette (GRA); Ward Broom (ATDC)

## Slide 3: Materials Development Takes Time
Teflon®
For coating
Nylon®
For abrasion resistance
Kevlar®
For protective clothing
Discovered by Ohio State University
First plant
New variants still coming out
1938
1950
Today
Marketing for cookware
1960
Discovered by DuPont
Went to department store
Parachutes & mosquito nets
Toothbrush, fishing line, tents, toys …
1930
1940
WW-II
Today
Discovered by DuPont
1,000,000th vest produced
1965
2014
Military uses
1978
22 years $1 Billion fines for environmental pollution
10 years
$500 Million R&D cost
13 years
$700 Million R&D cost
R&D, lab trials
Pilot production
Testing and scaling
Commercialization

## Slide 4: Too Vast to Search & Optimize
Polymer chemistry space
Homo/copolymers, commercial/ synthesizable/hypothetical polymers, neat resin, composites, crosslinked, etc.
Recipe/formulation space
Additives, curing agents, catalysts, solvent, reinforcements, mixing ratio, molecular weight, compatibilizers, etc.
Synthesis/processing space
Polymerization methods, curing conditions, mixing techniques, extrusion, injection molding, post-processing treatments, etc.

## Slide 5: Polymer Design with AI
Define screening criteria
Develop ML models to rapidly predict properties
Define search space and generate polymers
Screen and recommend candidates for experiments
Property | Target
Tg (K) | > 373
Td (K) | > 473
E (GPa) | > 2
𝛥H (kJ/mol) | -10 ~ -20
Data
Decision
Goal setting
Models
Predict/screen
Candidate design

## Slide 6
Designing Bioplastics
Tackling the crisis: a journey to sustainability

## Slide 7
540 PHAs
13 conventional polymers
14 PHA-based bioplastic candidates
Instant prediction for the key properties using multitask property predictors
1.4 million copolymers
PHAs
PHAs
Conventional polymers
PHAs
Search for polymers that meet the screening criteria
“Bioplastic design using multitask deep neural networks” Commun Mater 3, 96 (2022).
R
Christopher Künneth (University of Bayreuth, Faculty of Engineering Science) and Jessica Lalonde, Babetta L. Marrone, Carl N. Iverson, Rampi Ramprasad and Ghanshyam Pilania

## Slide 8
540 PHAs
13 conventional polymers
14 PHA-based bioplastic candidates
Instant prediction for the key properties using multitask property predictors
1.4 million copolymers
PHAs
PHAs
Conventional polymers
PHAs
Search for polymers that meet the screening criteria
“Bioplastic design using multitask deep neural networks” Commun Mater 3, 96 (2022).
Poor mechanical properties of PHAs
Large chemical space to search for the optimal copolymer
R

## Slide 9
540 PHAs
13 conventional polymers
14 PHA-based bioplastic candidates
Instant prediction for the key properties using multitask property predictors
1.4 million copolymers
PHAs
PHAs
Conventional polymers
PHAs
Search for polymers that meet the screening criteria
“Bioplastic design using multitask deep neural networks” Commun Mater 3, 96 (2022).
Solution - Utilize machine learning’s ability to rapidly canvas large search spaces
Thermal properties – Tg, Tm, Td,
Mechanical properties – YM (E), TS (σ), Elongation (ℇb) Gas permeabilities – O2, CO2, N2, He, CH4, H2
Model trained on 22,731 homo & co polymers

## Slide 10
540 PHAs
13 conventional polymers
14 PHA-based bioplastic candidates
Instant prediction for the key properties using multitask property predictors
1.4 million copolymers
PHAs
PHAs
Conventional polymers
PHAs
Search for polymers that meet the screening criteria
“Bioplastic design using multitask deep neural networks” Commun Mater 3, 96 (2022).
Solution - Utilize machine learning’s ability to rapidly canvas large search spaces
Thermal properties – Tg, Tm, Td,
Mechanical properties – YM (E), TS (σ), Elongation (ℇb) Gas permeabilities – O2, CO2, N2, He, CH4, H2
Model trained on 22,731 homo & co polymers

## Slide 11
“Bioplastic design using multitask deep neural networks” Commun Mater 3, 96 (2022).
Pipeline to design new PHA-based bioplastic candidates
540 PHAs
13 conventional polymers
14 PHA-based bioplastic candidates
1.4 million copolymers
PHAs
PHAs
Conventional polymers
PHAs
Instant prediction for the key properties using multitask property predictors
Search for polymers that meet the screening criteria

## Slide 12: 2 Candidates : Bio-replacements for PVC
PHAs
PHAs
Conventional polymers
PHAs
PVC
PHAs
PHAs
Conventional polymers
PHAs
“Bioplastic design using multitask deep neural networks” Commun Mater 3, 96 (2022).

## Slide 13: Bio-replacements
“Bioplastic design using multitask deep neural networks” Commun Mater 3, 96 (2022).
PE
PP
PVC
PET
PS
N6
PEN

## Slide 14
Designing PET-replacements
Can the new polymers surpass PET’s performance?

## Slide 15: PET – Polyethylene Terephthalate
Light weight, strong, good gas & moisture barrier properties
Broad range of use temperature -60 C – 130 C
Transparent (when quench processed)
Obtained by esterification (terephthalic acid + ethylene glycol) or trans-esterification (ethylene glycol + dimethyl terephthalate)

## Slide 16: Design Target
Design new polymers with property target criteria …
Target property | Proxy property | PET’s property (experimental) | PET’s property (predicted) | Goal (predicted)
Glass transition temperature (Tg) | Tg | 67 C – 81 C | 72 C | > 72 C
Transparency | Bandgap | 3.1 eV – 3.8 eV | 3.7 eV | > 3.7 eV
Transparency | Tendency to crystallize | 30% - 40% | 40% | < 40 %

## Slide 17: Procedure
ML models (Tg, bandgap, tendency to crystallize) used: Available at PolymRize™ (https://www.matmerize.com) and Polymer Genome (https://www.polymergenome.org)
Step 1
Generate candidate polymers
Step 2
Predict properties & screen candidates

## Slide 18: Approach for Generating Polymers
Reference polymer (PET) & reaction template
Polycondensation (Esterification)
New polymers inspired by the reference
Polycondensation
72 monomers from TSCA inventory
n
RA
168 monomers from TSCA inventory
n
RB
+nH2O
n
12,100 PET-like polymers
Can these polymers surpass PET?
RA
RB
SMARTS reaction template
[#8:1]=[#6:2][#8H:3].[#8H:4][#6:5] >>[#8:1]=[#6:2][#8:3][#6:5]
Diacid - PTA
CAS# 100-21-0
C1=CC(=CC=C1C(=O)O)C(=O)O
n
[#8:1]
[#6:2]
[#8H:3]
Diol - MEG
CAS# 107-21-1
C(CO)O
n
[#8H:4]
[#6:5]
+nH2O
n
PET
[#8:1]
[#6:2]
[#8:3]
[#6:5]
[#8:4]

## Slide 19: Promising Candidate PET Replacements
Predicted Tg (C)
Total 12,100 new polymer designs
Mean = 66.8 C
Standard dev. = 26.9 C
Minimum = -5.5 C
Maximum = 195.5 C
Pure PET
Predicted Tg = 72±15 C
Mean
Candidate polymers
Example polymers, Tg > 72 C
PET-*
#5003, Tg=123±23 C
#1427, Tg=153±22 C
#1454, Tg=100±18 C
#1362, Tg=102±26 C
#1456, Tg=75±17 C
#1413, Tg=75±17 C
#1595, Tg=122±22 C
#1259, Tg=149±29 C
Excellent
Exceptional
Better than PET
Comparable to PET
Confidential
Confidential
Confidential
PET-*
PET-*
Confidential
Confidential
PETG
Tritan
Ecozen
4,787 copolymers with Tg greater than PET’s Tg
#1456
#1413
#1454
#1362
#1595
#5003
#1259
#1427

## Slide 20: Screened Candidates
PET
Tendency to crystallize
15.9%
40%
>40%
1,108 polymers surpass PET’s Tg and bandgap with tendency to crystallize lower than 40%
Next step Experimental validation A few cases are handpicked, and being tested in the Ramprasad Research Group at Georgia Tech.
Tritan
Ecozen
“Designing PET-replacement copolymers using AI and virtual forward synthesis” in preparation

## Slide 21: Understanding Patterns and Correlations
Chi2n
-CH2- (not in a ring)
C3-C3-N3
c1cc(C)ccc1(C)
n(side chains, length<9 atoms)
n(rings in main chain)
C-C=C
SHAP value (Impact on Tg)
Feature value
Low
High
Feature
Tg (C)
Chi2n
-CH2- (not in a ring)
PC1
PC2
PC1
PC2
PC1
PC2
C3-C3-O1
C3-C3-O2
C3-C3-C3
C4-C3-O2
c1cc(C)ccc1(C)
n(rings in main chain)
C4-C4-C4
SHAP value (Impact on bandgap)
Feature
Feature value
Low
High
Bandgap (eV)
C3-C3-O1
C4-C3-O2
PC1
PC2
PC1
PC2
PC1
PC2

## Slide 22: Notable Polymer Informatics Ecosystems
Known polymer database
Hypothetical polymer database
Tools for polymer representation
Simulation tools
Fingerprinting scheme
Tools for visualization and statistics
AI tools for property prediction
AI tools for AI model training
Polymer Genome by Ramprasad Research Group https://www.polymergenome.org
Property prediction for neat resins (homo-, co-polymers)
PolymRize™ by Matmerize, Inc. https://polymrize.matmerize.com
Property prediction, model training, design for resin and complex formulations

## Slide 23
Matmerize creates new IP & databases
Matmerize develops PolymRize™
Established in 2021
Virtual PI assistant ASKPOLY
2010
Launched Polymer Genome Project sponsored by DOD
2015
Launched Polymer Genome for academic use
2024
2023
2020
Licensed polymer informatics IP exclusively to Matmerize by GTRC
Established in 2021 as a spin-out from the Ramprasad Group at Georgia Tech
Founded by Prof. Rampi Ramprasad and Dr. Chiho Kim
Built on more than a decade of pioneering AI technologies in polymer informatics
Co-founder
Prof. Rampi Ramprasad
Co-founder
Dr. Chiho Kim

## Slide 24: PolymRize™ Quick Views

## Slide 25: PolymRize™ Stock Models
Library of pre-trained models for polymer composites and neat polymers
Ready-to-use from day-1 for prediction, design/screening, and reinforced training
Solubility properties | Transport properties | Flammability properties | Electrical properties | Other properties
Hildebrand solubility parameter Solvent/non-solvent | Gas permeability Gas diffusivity Gas solubility Proton conductivity Water uptake Electrical conductivity | Time to ignition Peak heat release rate Average heat release rate Total heat release Optical smoke density Max. optical smoke density | Relative permittivity Electric strength | Limiting oxygen index
Electronic properties | Dielectric & optical properties | Thermal properties | Mechanical properties | Physical & thermodynamic
Bandgap Ionization energy Electron affinity | Dielectric constant Refractive index | Glass transition temperature Melting temperature Thermal decomposition temperature Coefficient of thermal expansion | Tensile strength Young’s modulus | Density Atomization energy Specific heat Fractional free volume
PolymRize™ Stock Models

## Slide 26: Thank You
Focuses on AI-assisted design of application-specific polymeric materials for:
Dielectric polymers for electrostatic energy storage
Polymers for fuel-cell applications
Polymers for Li-ion battery electrolytes
Membranes for gas separation
Membranes for organic liquid mixture separations
Conducting Conjugated polymers
Polymers for sustainable world
Nature Reviews Materials V9, p866–886, 2024
https://doi.org/10.1038/s41578-024-00708-8