## Slide 1
Carbon dioxide information analysis center, Oak Ridge National Lab.
Photo: Guardian, Alex Ford.
Sokseiha Muy and Yang Shao-Horn
Accelerating Electrolyte Discovery with AI: High-Throughput screening of multi-component Li and Na electrolytes for battery applications

## Slide 2: Decarbonizing the transportation sector
In its Net-zero-by-2050 emission roadmap, the IEA projects the annual battery demand to reach 6.6 TWh in 2030 and 14 TWh in 2050
Require massive investment in electricity storage technology that is cost-effective and highly efficient.
https://www.iea.org/reports/net-zero-by-2050

## Slide 3: From Li-ion to Na-metal batteries
https://ev-database.org/cheatsheet/range-electric-car
Current LIB technology with graphite anode has limited
energy density ~ 250 Wh/kg which translates into a
maximum driving range ~ 600 km
Replacing Li and graphite by Na can increase the energy density and lower the cost
Na metal, being more reactive than graphite, require a new electrolyte for stable cycling.
Li-ion battery
Na metal battery
J. Janek et al., Nat. Energy., 1, 16141, 2016

## Slide 4
Leveraging AI and HT experiment to efficiently navigate chemical space
NaTFSI
12 organic solvents
NaFSI
Temperatures
25
80 ºC
40
60
Na electrolyte database
Number of solvents
1
12
NaOTf
NaPF6
5 salts
Total concentration
0.05
2 M
Total concentration
0.05
Salts ratio
Solvents ratio
> 1014
possible combinations
Liquid chemical space
Number of salts
1
5
NaClO4
Courtesy of Dr. Vanesa Munoz Perales

## Slide 5: Optimizing the robotics workflow for liquids and polymers
Creating the design
45 formulations
x4 EIS setups
EIS measurements and fittings
Ionic conductivity
Assemble liquid cells
Re (Z) / Ω
-Im (Z) / Ω
96 formulations
Cast and dry films
Assemble polymer cells
Film quality and thickness
Dispense
Liquid electrolytes
Polymer electrolytes
100 new formulations in 5 days
50 new formulations in 5 days
Courtesy of Dr. Vanesa Munoz Perales

## Slide 6: The largest database of Na electrolytes
We envision having 10 000 datapoints by the end of 2025
2240 datapoints from our robot.
560 unique formulations at 4 temperatures.
Only Na electrolytes
12 solvents, 5 salts
Other solvents and salts will be added
Courtesy of Dr. Vanesa Munoz Perales

## Slide 7: Li-Electrolyte Databases
K. Ritesh et al., Chem. Mater., 37, 2720, 2025.
B. Qiao et al. ACS Cent. Sci., 6, 1115, 2020.
CALiSol-23
Chicago
13267 datapoints mined from
the literature
Only Li electrolytes
38 solvents and 14 salts
10143 datapoints mined from
the literature
8187 Li-electrolytes datapoints
202 solvents and 73 ‘salts’
P.D. Blasio et al., Scientific Data, 11, 750, 2024.
In-house
~100 datapoints of PEO-based
oligomers

## Slide 8: ML: schematic of the Neural Network Architecture
Encoding
Block
Fitting
Block
[Li+]
F[P-](F)(F)(F)(F)F
FC1COC(=O)O1
Heid et al., J. Chem. Inf. Model, 9, 64, 2024.

## Slide 9: ML model trained on Calisol database

## Slide 10: Transfer learning to Na electrolytes
The encoding blocked of the solvents and anions are ‘locked’ and only the fitting block and the encoding block of the cation are allowed to adjust during training.

## Slide 11: ML trained on combined CALiSol-23 and Na electrolyte databases
Li electrolytes
Na electrolytes

## Slide 12: Ongoing work: Combine with Polymer Electrolyte Databases
G. Bradford et al., ACS Cent. Sci., 9, 206, 2023

## Slide 13: ML model trained on combined Calisol and polymers databases
Li liquid electrolytes
Li polymer electrolytes

## Slide 14: Toward a General AI Model for Ionic Conductivity in Liquid, Polymer, and Solid Electrolytes
C.J. Hargreaves et al., npj Comput. Mater., 9, 9 (2023)
S. Wang et al., Chem. Mater., 36, 11541, 2024

## Slide 15: Future outlook: Leveraging computational databases
OMol25: The largest open computational database to date with ~ 83 millions molecular systems
https://arxiv.org/pdf/2505.08762
https://molecular-universe.ses.ai
SES Molecular Universe: 100 million molecules.
Only solvents. Only 1 million molecules accessible through the free version.

## Slide 16: Acknowledgement

## Slide 17: Back-up slides

## Slide 18: Developing an efficient and automated workflow
K. Ritesh et al., Chem. Mater., 37, 2720, 2025.
P.D. Blasio et al., Scientific Data, 11, 750, 2024.

## Slide 19
High-throughput methodology – “high entropy” electrolytes – Breakthrough Energy Explorer Fellow
Goal 1: Identify promising high conductivity electrolytes using high-throughput experimentation and machine learning.
N = 1, 2, 3, … n
Goal 2: Measure various entropies of electrolytes and correlate to ionic conductivity and composition.

## Slide 20
Parallel Session A: AI-Driven Materials Discovery, Energy Systems, and Computational Modeling

## Slide 22: Examples of salts used in Chicago database

## Slide 23: Ionic conductivity

## Slide 24: Solvents and Salts

## Slide 25: ML model
Based on message-passing graph convolutional neural network as implemented in the Chemprop package.
Similar to the one used in Chibueze’s paper
Heid et al., J. Chem. Inf. Model, 9, 64, 2024.

## Slide 26: Next steps
Improve the accuracy of models:
  Including more data
  Finetuning the hyperparameters
  Testing new model architectures (taken into account the 3D coordinates of the molecules)
Transfer learning to Na-database
Importance analysis

## Slide 27
~30 slides with 5 slides of general intro.
ML/AI, protein structure?/drug discovery
Al/ML discovery of materials.
Progress/contra
Nature, google and Berkeley, as well as Nature from Tian Xie?
Bo’s work changing PEO, Gab’s polymer paper, Chibueze
Robot’s role