## Slide 1: Tuning Soft Magnetic Properties in Fe-Based Nanocrystalline Alloys via Ge Substitution
Paul W. White
Tula R. Paudel
Department of Physics
South Dakota School of Mines and Technology
Rapid City, South Dakota

## Slide 2: collaborators
Tula R. Paudel (SDSM&T Physics Department)
Nick Bruno (Glenn Research Center)
Jacob Peterson (SDSM&T, EMES Research Scientist)
Eli Meakins (Mechancial Engineering Masters Student, Graduated)
Parashu Kharel (SDSU Physics Department)

## Slide 3: outline
Background
  Amorphous Materials
  Machine Learning Force Fields in VASP
Hybrid method of generating amorphous structures
Magnetic properties of Fe-Nb-Cu-Si-Ge-B
  DFT Results
  Magnetization from VSM
  p-d hybridization of Fe-Si and Fe-Ge
Conclusions

## Slide 4
Amorphous Materials

## Slide 5: Amorphous vs crystalline
Crystalline: long-range order from repeating unit cells
Amorphous: lacks long-range ordering
If formed from a supercooled liquid, it can be referred to as a glass
Nanocrystalline alloys contain both

## Slide 6: Ferromagnetic metallic glasses
Contain (Fe, Co, Ni)
Make excellent soft magnets
  High magnetic saturation, high magnetic permeability, low magnetic coercivity

## Slide 7: High efficiency inductors
Electric propulsion systems need increased power density
Half of the weight of an advanced motor controller is the filter inductor
Needs to operate at high frequencies (>50kHz)
High magnetic saturation (>0.8T)
Low power losses, combination of eddy currents and hysteresis losses

## Slide 8: Making a metallic glass ribbon
Set crucible 10 from Cu-wheel
Pump chamber to vacuum and fill with Ar
Melt ingot using induction heating
Eject liquid metal onto Cu-wheel
Achieves ~106 cooling rate

## Slide 9
VASP ‘on-the-fly’ Machine Learning Force Fields
White, Paul W., et al. Journal of Non-Crystalline Solids, vol. 647, Jan. 2025, p. 123283, https://doi.org/10.1016/j.jnoncrysol.2024.123283.

## Slide 10: AIMD Simulations with MLFFs
Ab-initio molecular dynamics (AIMD) vs classical molecular dynamics
  AIMD uses density functional theory (DFT) to solve for the interatomic forces
  Classical MD uses the gradient of a predetermined interatomic potential to calculate interatomic forces (LAMMPS)
DFT is costly to do
  Employ machine learning force fields (MLFF) to accelerate the AIMD
  MLFF is trained by the structure, energies, forces, and stresses evaluated during AIMD calculations
  When to use the MLFF is determined by the Bayesian linear regression which predicts the uncertainties of using the MLFF

## Slide 11: How MLFFs work
Total energy is the sum of local energies
Local energy is a function of the local environment (Key Assumption!)
Energies, forces and stress tensor are simultaneously fitted by one local energy function(al)

## Slide 12: Descriptors
r
i
j
i
k
j
Radial Descriptor
Angular Descriptor
r
s
Local environment can be described by radial and angular distribution functions

## Slide 13: Descriptor functions
Radial and angular distribution functions are written as
, denote expansion coefficients
Up to 1000 coefficients for each atom, and is a non-linear function!
n, l, and m denote radial numbers, angular numbers and magnetic quantum numbers respectively

## Slide 14: Kernel Trick
It is now convenient to express the local potential energy of atom i in structure in terms of linear coefficients and a Kernel
The Kernel contains all of our coefficients ,
Structure x
x1
x4
Observable
Adjust , , ,…, to get peak heights

## Slide 15: ‘on-the-fly’ MLFF
Bayesian linear regression is used to predict the error of the MLLF if the MLFF were to be used
If the error is above a user defined threshold first principles is used otherwise the MLFF is used
When a first principles calculation is done the results are added to the training data
The MLFF is NOT refit every time, only when the error is above a second separate threshold

## Slide 16: Verification of the MLFF
Check how accurately the MLFF can predict energy, forces, and stresses of the training data
The error is extremely small
16

## Slide 17
Hybrid Method for Generating Amorphous Structures
White, Paul W., et al. Journal of Non-Crystalline Solids, vol. 647, Jan. 2025, p. 123283, https://doi.org/10.1016/j.jnoncrysol.2024.123283.

## Slide 18: Generating amorphous structures
Randomly insert 100 atoms into a box
Equilibrate the initial random structure at 300K (NPT) for 20ps using ab-initio molecular dynamics
Hold the equilibrated structure at 300K for an additional 5ps, sampling a structure every 50fs, a total of 100 new structures
Only ~450 first-principles calculations were done for 20,000 total steps

## Slide 19: Check Amorphousness
X-ray diffraction of experimental measurement and simulated patterns match

## Slide 20: Voronoi analysis
Draw a line to all nearest neighbors
At the midpoint, draw a plane perpendicular to the line
Intersections of planes create the edges and vertices of the Voronoi polyhedra

## Slide 21: Generated structures are unique
Voronoi analysis shows us that the local configuration changes from structure to structure
Pentagons are the most common which is a sign of amorphousness

## Slide 22
Magnetic properties of Fe72Nb4Cu1Si16-xGexB7
(x=0-8) at %

## Slide 23: X-ray diffraction of ge samples
XRD shows that the casted ribbons are amorphous and contain no crystallinity
EDS shows samples are homogenous at the microscale

## Slide 24: Magnetization from vsm
High magnetic saturation
Increases with Ge concentration
Dr. Parashu Kharel

## Slide 25: Magnetization from dft
Increase in magnetization with Ge
Predicts a plateau in magnetization above 12% Ge, which we have not been able to synthesize

## Slide 26: Fe-ge hybridization
Stronger hybridization between Fe-Ge increases magnetization

## Slide 27: Conclusions
The hybrid method for generating amorphous structures is efficient and reliable
Mechanical and magnetic properties can be calculated from this method
Magnetization agrees with experimental results and can explain the increase in magnetization through increased p-d hybridization of Ge-Fe
White, Paul W., et al. Journal of Non-Crystalline Solids, vol. 647, Jan. 2025, p. 123283, https://doi.org/10.1016/j.jnoncrysol.2024.123283.