## Slide 1
Khimananda Acharya
Alexey Lipatov
Tula R. Paudel
Workshop for AI-Powered Materials Discovery at Great Plains, USD
June 23, 2025
Charge Carrier Modulation in Cr₂TiC₂Tx MXene: A Promising Material for Future Technology

## Slide 2: Outlines
1
CURIOUS
SMART
TENACIOUS
2D Materials
MXene Background
Electrical measurement
Structure Optimization
P-/n- tunable conductivity
Conclusion

## Slide 3: 2D materials
1
Atomically thin layers: Strong in-plane covalent bonds, weak interlayer van der Waals interactions
Andre Greim and Konstantin Novoselov 2004
They got Nobel prize in physics in 2010
Graphite
Graphene
Currently, we have vast number of 2D materials beyond graphene
3 D
2 D
Notes: Let’s begin with 2D materials.
What you see here is a regular pencil made of graphite. But if we zoom in under a microscope, we can find that graphite is made of many stacked layers of carbon atoms, which is one of the first and most famous 2D materials.
2. What makes these materials special is their bonding. Within the layers, the atoms are strongly connected by covalent bonds, but between the layers, they’re only loosely held together by van der Waals forces. That’s why it’s possible to separate them into atomically thin sheets.
This was first done in 2004 by Andre Geim and Konstantin Novoselov, using a surprisingly simple method—just scotch tape! For this discovery, they were awarded the Nobel Prize in Physics in 2010.
But graphene was just the beginning. Today, we have a huge variety of 2D materials, each with exciting properties—way beyond just graphene.

## Slide 4: Beyond Graphene
1
vdW
vdW
Bagheri, S., ...,Acharya, K. et. al. Matter, (2024).
vdW
Acharya, K., et. al., Physical Review B, (2025).
vdW
Lu, H. , Acharya, K, et. al. Advanced Functional Materials, (2024).
vdW
Today’s talk
Notes: 2D materials are not limited to single atomic layers.
This center illustration shows several 2D materials that I have already worked on or am currently working with. Let me walk you through some examples.

## Slide 5: Background/Motivation
1
CURIOUS
SMART
TENACIOUS
The first MXene (Ti3C2Tx) was discovered at Drexel University in 2011
Over 50 MXenes have been synthesized to date with many more predicted theoretically
Potential applications : Batteries, electronics, medical devices, and more
VahidMohammadi, A., Rosen, J., & Gogotsi, Y. (2021) Science
Tunable compositions and exhibit rich surface chemistry
MXenes are a class of two-dimensional inorganic compounds
Notes: MXenes were first discovered in 2011 at Drexel University. Since then, over 50 types have been created, with even more predicted.
What makes them special is their wide range of applications: from batteries and electronics, to biomedicine, sensors, smart textiles, and even 5G antennas.
They’re strong, conductive, and versatile – making them one of the most promising families of 2D materials today.

## Slide 6: MAX Phase
1
CURIOUS
SMART
TENACIOUS
MAX phases are layered hexagonal carbides and nitrides which have the general formula: Mn+1AXn
MXene= MX (MAX)+ ene (graphene like)
n=1 to 4
M= transition metal
A= IIIA or IVA group
X= carbon, nitrogen
Mn+1AXn
https://en.wikipedia.org/wiki/MAX_phases

## Slide 7: MXene Structure
1
-OH ,-F, -O, -Cl
Surface Functional Groups
Etching
Mn+1XnTx
Sonication
Mn+1AXn
CURIOUS
SMART
TENACIOUS
Monolayer
n=1 to 4
M= transition metal
A= IIIA or IVA group
X= carbon, nitrogen
MAX MXene
Mn+1XnTx
Notes: Now you might be wondering—how are MXenes made? They actually come from a another material called a MAX phase. You can see it here on the left.
To make MXenes, we use a chemical process to selectively remove the A layer. What’s left is a thin, layered structure called a MXene, with surfaces often terminated with oxygen, fluorine, or hydroxyl groups.

## Slide 8: Background/Motivation
1
CURIOUS
SMART
TENACIOUS
Single transition metal:
2-1 MXenes (Ti2CTx), 3-2 MXenes (Ti3C2Tx), 4-3 MXenes (Ti4N3Tx) 5-4 MXenes (Mo4VC4Tx)
Double transition metal:
2-1-2 MXenes (Cr2TiC2Tx), 2-2-3 MXenes (Mo2Ti2C3Tx)
Types
This Work
It has more tunability due to two transition metal
It has magnetic property besides other MXenes
Many possibility???
-OH ,-F, -O, -Cl
Surface Functional Groups
MAX
MXene
AI/Machine Learning
Notes: We can have MXenes with either single or double transition metals.
Because of its magnetic property, this MXene offers more functionality for electronic devices
So based on this motivation, we selected a double transition metal MXene—Cr₂TiC₂Tₓ
Our collaborators synthesized high-quality Cr₂TiC₂Tₓ flakes and also carried out the electrical measurements

## Slide 9
1
CURIOUS
SMART
TENACIOUS
Previous studies produced sub-1- sheets of
We report the synthesis of high-quality monolayers with lateral sizes exceeding 15 for single-flake measurements
Notes: HRTEM (High-Resolution Transmission Electron Microscopy) and SAED (Selected Area Electron Diffraction)

## Slide 10: Electrical Measurement
1
CURIOUS
SMART
TENACIOUS
First time reported p-type conductivity and semiconducting
Linear
Positive photoresponse
Schematic of FET Device
But!! MXene known for metallic behavior with high concentration carrier
devices were measured in a Lake Shore TTPX cryogenic probe station at a base pressure of about Torr.
p-type conductivity
n = 5.25 ± 0.17×1021 cm-3
AFM image
Au
Au
MXene
Si/SiO2
Notes: FET devices based on Cr2TiC2Tx as the channel material, conductive p-doped Si as the global back gate, 300-nm thermally grown SiO2 as the gate dielectric, and Cr/Au electrodes, which were fabricated using the e-beam lithography technique.
P-type conductivity: Indicating that holes are the major charge carriers
3. Positive photoresponse: Semiconducting nature
4. For a p-type semiconductor:
A negative gate voltage attracts holes to the channel, increasing their density and improving conduction, leading to a higher I_D.
A positive gate voltage repels holes from the channel, reducing their density and making conduction more difficult, leading to a lower I_D.

## Slide 11: DFT Work Motivation
1
CURIOUS
SMART
TENACIOUS
A quantum mechanical method that uses electron density
Vienna Ab Initio Simulation Package (VASP) for DFT calculations
DFT Calculations:
Is Cr₂TiC₂Tₓ really a p-type semiconductor?
Can it also exhibit n-type or metallic behavior?
Questions:
Hubbard U = 4 eV for Cr 3d orbitals and 3 eV for Ti 3d
GGA approximation with 540 eV energy cutoff
DFT-D3 van der Waals correction is used

## Slide 12: Optimizing Crystal Structure
1
CURIOUS
SMART
TENACIOUS
Lattice Parameters
Surface functional groups (–O, –F, –OH) were placed on energetically favorable hollow sites, right above the Ti atoms
These optimized structures were used for further analysis
-OH ,-F, -O, -Cl
Notes: In-plane lattice parameter obtained by lowest energy from ‘E’ Vs ‘a’ plot

## Slide 13: Optimizing Crystal Structure
1
CURIOUS
SMART
TENACIOUS
Role of Surface Functional Group (Tx)
Role of Cr vacancy ( )
Oxygen substituting Carbon ( )
-OH ,-F, -O, -Cl
Ti
Cr
C
Cr atoms are exposed on the outer surface during etching, making them susceptible to being etched away.
Formation of oxycarbides is possible, as indicated by Michałowski et al., Nature Nanotechnology (2022)
Notes: In-plane lattice parameter obtained by lowest energy from ‘E’ Vs ‘a’ plot

## Slide 14: Different functional group
1
CURIOUS
SMART
TENACIOUS
Role of Surface Functional Group (Tx)
Role of Cr vacancy ( )
Oxygen substituting Carbon ( )
Notes: In-plane lattice parameter obtained by lowest energy from ‘E’ Vs ‘a’ plot

## Slide 15: Different functional group
1
CURIOUS
SMART
TENACIOUS
DOS for (T= -F, OH and O)
Pristine is either p type conducting, or just semiconductor
always gives p-type
+ Cr Vacancy
Notes: 1. We considered the effect of individual (–O, –F, and –OH) functional groups and their equal mixtures: –O/–F and –F/–OH.
2. Cr vacancies at 1.67 atom % (corresponding to 2 vacancies in a 120-atom supercell) is used for all structure
3. O or a mix of O and F - p-type and OH, and F or mix of OH and F --- semiconducting

## Slide 16
1
CURIOUS
SMART
TENACIOUS
Role of Surface Functional Group (Tx)
Role of Cr vacancy ( )
Oxygen substituting Carbon ( )
Notes: In-plane lattice parameter obtained by lowest energy from ‘E’ Vs ‘a’ plot

## Slide 17: p-/n tunability with oxygen substitution
1
CURIOUS
SMART
TENACIOUS
We fixed –O, –OH, and –F surface functional groups in a 1:2:5 ratio
Smaller is p-type semiconductor
Larger is n-type semiconductor
DOS of
Michałowski et al., 2022, Nature Nanotechnology
25%
12.5%
6.25%
4.16%
0%
Notes: 1. We fixed –O, –OH, and –F surface functional groups in a 1:2:5 ratio1, which is approximately similar to that determined in a recent SIMS measurement.
2. Different percentages of O substituting C (Oc) is used.
3. Cr vacancies at 1.67 atom % is used for all structure.

## Slide 18: Tunable p-/n- conductivity
1
CURIOUS
SMART
TENACIOUS
promotes the p-type character, while promotes the n-type character
p-/n- type conductivity is tunable in

## Slide 19: MXene with AI/ML
1
CURIOUS
SMART
TENACIOUS
Enormous configurational space: different transition metals, surface terminations, and stacking orders
Traditional DFT/Experimental measurement can't explore every possible structure due to high computational cost
Infinite possibility???
-OH ,-F, -O, -Cl
Surface Functional Groups
MAX
MXene
Current Challenge:
AI/Machine Learning:
Can predict key material properties (e.g., bandgap, conductivity type etc.) without relying on expensive DFT calculations for every configuration.
Successfully applied to MXenes to predict properties like work function based on surface terminations and composition (e.g., Roy et al., J. Phys.: Energy, 2021).
Notes: We can have MXenes with either single or double transition metals.
Because of its magnetic property, this MXene offers more functionality for electronic devices
So based on this motivation, we selected a double transition metal MXene—Cr₂TiC₂Tₓ
Our collaborators synthesized high-quality Cr₂TiC₂Tₓ flakes and also carried out the electrical measurements

## Slide 20: Summary
1
CURIOUS
SMART
TENACIOUS
Is Cr₂TiC₂Tₓ really a p-type semiconductor? Yes
Can it also exhibit n-type or metallic behavior? Yes
Questions:
Redefining MXene boundary
Pristine demonstrates p-type conductivity, which is the first reported for any MXene so far.
The p/n-type conductivity is tunable, depending on transition metal vacancies and oxygen substitutions.
Similar tunability is expected for other double-transition-metal MXenes.
Beyond the traditional metallic behavior.

## Slide 21: Acknowledgement
1
CURIOUS
SMART
TENACIOUS
Bagheri, S., Loes, M. J., Lipatov, A., Acharya, K., Paudel, T. R., Lu, H., ... & Sinitskii, A. (2024). Synthesis of high-quality large Cr2TiC2Tx MXene monolayers, their mechanical properties, p-type electrical transport, and positive photoresponse. Matter, 7(12), 4281-4296.
Collaborator
QR code for paper
Notes: Big thanks to our collaborators and funding sources, especially South Dakota Mines, NSF, and others.

## Slide 22: THANK YOU
1
CURIOUS
SMART
TENACIOUS
Any Questions??

## Slide 23
Extra Slides

## Slide 24
vdW
CrI2
vdW

## Slide 25
🧬 Biomedicine
Why MXenes? They are biocompatible and can be functionalized for drug delivery, imaging, or even killing cancer cells via photothermal therapy.
🧪 Sensors
Why MXenes? MXenes respond quickly to gases, chemicals, and physical changes due to their high surface area and conductivity—perfect for sensitive sensors.
📶 Electromagnetic Interference (EMI) Shielding and Antennas
Why MXenes? MXenes block electromagnetic waves effectively due to their metallic nature and layered structure—useful in shielding electronics and making compact antennas.
💡 Optoelectronics
Why MXenes? They can absorb and conduct light and electricity, making them useful in solar cells, LEDs, and transparent electrodes.
🌍 Environmental
Why MXenes? MXenes can adsorb toxic metals, dyes, and pollutants thanks to their surface chemistry—ideal for water and air purification.
📱 5G Antennas, Electronics, Smart Textiles
Why MXenes? Their flexibility, conductivity, and printability make them ideal for wearable electronics and high-speed communication devices like 5G antennas.
🔋 Energy Storage and Harvesting
Why MXenes? MXenes have high electrical conductivity and a layered structure, which allows fast ion movement—perfect for batteries and supercapacitors.

## Slide 26
Graphene
MXenes
h-BN
PVK-Br
Graphene
MXenes
h-BN
PVK-Br
V